## Slide 1
Alexander Romanenko
Intersections between Nuclear Physics and Quantum Information
30 March 2018
Ultra-high Q superconducting cavities from accelerators for increased coherence of 3D quantum systems

## Slide 2: Outline
Superconducting RF (SRF) cavities in particle accelerators
Appeal of SRF cavities for quantum systems
  Ultra-high Q > 1010 factors are routine
  Decades of expertise in surface engineering and underlying superconducting RF science
Progress towards the “quantum” implementation at FNAL
  Clarification of the TLS role
  First measurements at T < 20 mK

## Slide 3: How are Particles Accelerated in Modern Machines?
Superconducting radiofrequency (SRF) cavities
High quality EM resonators: Typical Q0 > 1010
Over billions of cycles, large electric field generated
Particle beam gains energy as it passes through
Slowed down by factor of approximately 4x109
Input RF power at 1.3 GHz
~1 m
Images from linearcollider.org, WIkipedia
Notes: say like RLC circuit, Point out currents on surface, with small R because it is superconducting

## Slide 4: Modern large scale accelerators are based on SRF
European XFEL
LCLS-II at SLAC
Fermilab is building half (17+) of cryomodules
Q > 2.7 x 1010 @ 2K, 16 MV/m
~1000 cavities
Specification:
Q > 1010 @ 2K, 23.6 MV/m

## Slide 5: Quantum Computing: 3D circuit QED architecture
H. Paik et al, Phys. Rev. Lett. 117, 251502 (2016)
Machined Aluminum host cavity
State-of-the-art quality factors Q in quantum computing are ~108

## Slide 6: High Q SRF cavities for improved coherence
Q > 1011
1-cell Fermilab cavities of various frequencies
Q ~ 108
M. H. Devoret and R. J. Schoelkopf, Science 339, 1169–1174 (2013)
Potential of up to ~10 seconds of coherence

## Slide 7: RF Penetration Layer drives the performance
RF fields
Helium cooling
RF currents
~100 nm
Niobium ~3 mm
RF fields
Image from linearcollider.org
<0.1% of thickness
Engineering the surface layer is crucial to performance

## Slide 8: Major SRF Infrastructure at Fermilab (necessary to achieve high performance/high Q)
electropolishing
tuning
Class 10 clean room/high pressure
water rinsing
clean room assembly
Furnace treatment

## Slide 9
Can we translate high Q expertise in SRF cavities to ‘quantum regime’?
First task: what is the cause of the low field Q slope and what happens with Q as we decrease the field further?
Second task: what happens at lowest T < 20 mK?

## Slide 10: Renewed importance of the low field Q slope
A. Romanenko et al, Appl. Phys. Lett. 105, 234103 (2014)
1.3 GHz
1.5K
How will the best cavities we have behave at ultralow fields for various possible applications?
Quantum computing/memory
Dark sector searches
Gravitational effects
….

## Slide 11: Saturation of Q decrease
T=1.5K
Now measured down to
<N> ~ 1000 photons
Good news: low field Q saturates at Q>3 x 1010
1.3 GHz
A. Romanenko and D. I. Schuster, Phys . Rev. Lett. 119, 264801 (2017)

## Slide 12: Direct probing in the new regime with single cell cavities
f = 1.3 GHz, TM010 mode

## Slide 13: Single shot measurements
Q > 1010 cannot be measured using standard network analyzer techniques
Instead -> decays from PLL state with bandpass filtering (10-1000 Hz around resonance) instead
QL=2pft

## Slide 14: Various cavities/surface treatments investigated
Changes within penetration depth have little effect
Oxide growth/change -> strong increase in very low field dissipation

## Slide 15: From 2D resonator world
J. Gao, PhD Thesis, Caltech, 2008
J. Zmuidzinas, Annu. Rev. Condens. Matter Phys. 2012. 3:169–214
Two level systems in the dielectric as a cause

## Slide 16: Two level systems in the natural niobium oxide?
According to Martinis et al, Phys. Rev. Lett. 95, 210503 (2005) -> electric field effect
Nb
Nb2O5
5 nm
Nb
Nb2O5
100 nm
A. Romanenko and D. I. Schuster, Phys . Rev. Lett. 119, 264801 (2017)

## Slide 17
What happens at lowest T < 20 mK, low powers?

## Slide 18
2.6 GHz 1-cell cavity

## Slide 19: First try: Q at T ~ 12 mK, down to ~1000 photons
Q ~ 2 x 109
Publication with full details in preparation
E ~ 1000 photons
t ~ 100 ms : >10x better than previous records

## Slide 20: Immediate plans
Couple a very high Q SRF cavity with the transmon qubit to probe the achievable coherence times
Collaborations with:
Univ. of Wisconsin (Madison):
Prof. Robert McDermott
Chris Wilen
NIST: D. Pappas

## Slide 21: Summary
Accelerator ultra-high Q microwave 3D cavity expertise can enable a qualitative jump on achievable photon lifetimes/coherence
  Complex accelerators with hundreds of Q > 1010 cavities are routine, Q >1011 is the state-of-the-art
Very high Qs can be translated to ”quantum” regime
  Demonstrated Q ~ 2 x 109, t ~ 100 msec at 12 mK, 1000 photons at the first try
First 3D-SRF qubits are to be tested shortly